USE OF CHROME SPRAY KIT

2 . Basecoat Application :

If using CB-7 Basecoat

Apply 2 coats of CB-7 base coat catalyzed 50% with CCB-7 
Let air dry 48 hours, at room temp.
If using CB-5 Basecoat

Apply 2 coats of the New CB-5 mixed 15% with CCB-5. Drying at 60 ° C for 3 hours. For this product is REQUIRED using oven drying

2 . Chrome Application :
- Apply the Preactivator with the Preactivator SPRAY , 8% mixed with distilled water (you can do the mixing in the same spray) , until it covers the entire surface. 
You can use the same water that is inside the distilled water Pump Spray 
- Rinse with Pump Spray distilled water
- Apply the Activator with the Activator SPRAY prepared 2% with distilled water (do the mixing in the same spray) prepare it the day after.
You can use the same water that is inside the distilled water Pump Pressurre Spray
- Rinse with Pump Spray distilled water
- Fill the Component A and Component B. Do not fill more than half spray. Chrome with both SPRAY PUMPS A/B.

Keep chroming until you cover the entire surface. 
- Rinse with Pump Spray distilled water
- Dry the entire piece (with a hairdyer, or in the oven)
It is recommended to dry in the oven for 30-45 minutes at 40 ° C maximum and let cool down before topcoating

3 . Apply CF-4 topcoat catalyzed 20% with CCF- 4 and 20% Solvent DS with a regular spray gun.

# Text boxes

Wath the instructional video for more information